Powdermill 2010

Early tests done without background = Rossler config 1; others tests with background = Rossler config 3

Company/material name	Threat Score	      Reflectance of Surface 1         IGU?

Certoplast tape on glass

10V

1” white vertical stripes spaced 4” edge to edge

No background, low sample size

Threat score 4

10H		1” white horizontal stripes spaced 4” edge to edge

No background

Threat score 21

Evonik

PLEXIGLAS SOUNDSTOP® GS CC	9	         10				n0

(black h plexi)

2mm embedded polyamide threads, spaced 28mm

(low sample size)

Viracon Glass  Dot/Hole series

5065: 20% Coverage			22		11%				yes

1/8” dots;  no background

5065: 20% Coverage			41		11%				yes

1/8” dots;  with background

5006: 40% Coverage		24		11%				yes

1/8” dots no background

Line Series

2256: 20% Coverage

1/8” lines

6	           11%				yes

Custom: 20% coverage

1/8” lines

10                    11%				yes

Company/material name		Threat Score	      Reflectance of Surface 1   IGU?

CYRO Industries plexiglas

80% UV reflecting Plexiglas		52	8% in non-UV wavelengths		no

No visible pattern

Window Alert

2x7

3.5” decals spaced 3.6” x 2”

Threat score no background 18

Threat score with background 24

3x7		3.5” decals spaced 2.5” x 2”

Threat score no background 3

3x13

3.5”x0.9” decals spaced 2.5”x2”

Threat score  no background 8

2x13							3.5”x0.9” decals spaced 3.6”x2”

Threat score  no background 26

Company/material name		Threat Score	      Reflectance of Surface 1   IGU?

Luremaking

UV Blast paint (reflects 14% UV)      no background

2” stripes 2” apart			39		variable			no

As above, on UV			26		variable			no

absorbing film

2” stripes alternating

with 2” absorbing stripes		14		variable			no

Solutia window film

No background

UV Pattern prototype		17		variable			no

2” reflecting stripes x 2” absorbing stripes

Photo taken with UV camera (not our pattern)

Arnold Glass

Ornilux Mikado N33 Advance

Mikado (no background)		42		16				yes

Mikado (with background)		34		16				yes

These Mikado trials done using Arnold IGU control, visually different from plain glass, so these data not comparable (but huge sample sizes)  and not used in LEED table

Company/material name		Threat Score	      Reflectance of Surface 1   IGU?

SurfaceCare/Solyx?

2 mm grey stripes spaced 28 mm

30		variable			no

Small sample size; Field data would predict better score

2011

Tunnel turntable starting to list and becoming harder to turn…..

Company/material name		Score	      Reflectance of Surface 1   Insulated Glass?

Chart tape on glass, all with no background

.25” wide white vertical stripes spaced 4” (10V) Threat score 9

.25” wide white vertical stripes spaced 3” Threat score 17 (??)

.25” white horizontal stripes spaced 4”Threat score 11

.25” white stripes spaced 4” 72.5 degrees  Threat score 5

.25” white stripes spaced 4” 45 degrees Threat score 8

1/8” black horizontal stripes spaced 1”Threat score 7

1/8” black vertical stripes spaced 2” Threat score 6

Arnold Glass

Grid

Threat score 45

(probably random)

Not tested

Lots of dots

Threat score  68

(attracting birds)

2012

Guardian Glass

Photovoltaic Grey Crystal		23		        6% 				yes

Not commercially available

Tested with background

Walker Glass tested with background

Reversed dots

threat score 39

Fine mesh

Threat score 36.5

211/Continuous stripe

3 3” spacing

Threat score 28

(2013 score 34)

Velour

threat score 35

Arnold Glass

Unit 2 (commercially available – solar control glass)

Outside: 6mm Float Scandic (THIS SIDE IS OUTSIDE)

Cavity: 16mm spacer

Inside: 8mm laminated Float mikado (0.76 PVB)

threat score 23

Unit 7 (same configuration previously tested at Powdermill, commercially available, version in original LEED table) Mikado N33 Advance

Outside: 4mm Float mikado (non-tempered) (THIS SIDE IS OUTSIDE)

Cavity: 16mm spacer

Inside: 8mm laminated Float N33 (0.76 PVB)

Score 2012: 72.9	Trials: 85		WRONG! SHOULDN’T USE 2010 DATA,

Score 2010: 66.3	Trials:169		NEED TO CHANGE ORNILUX SCORE IN

Composite score: 68.5			TABLE

Threat score 27

Unit 8: Laminated Screen Print on surface 1

White, vertical stripe; 3mm stripe / 15 mm space

Score 2012: insufficient trials (33)

Score 2011: 71.3 Trials: 94

Composite score: 73.2

Threat score 27		n/a				no

Unit F12-8: 12 mm triple laminate guardrail glass

Tested without background

3 x’s 4 mm float; 2 x’s Mikado; 2 x’s 0.76 mm PVB

Threat score 52  Trials: 100

ALSO TESTED Ten ARNOLD IGU PROTOTYPES

2013

Walker Glass

Etched  glass patterns

5??/Continuous stripe

3” spacing

Threat score 34

511/ Barcodes

Threat score 43

vertical lines variously 1/16" to 3/16" wide,

spaced variously  3/16" to 5/8" apart,

staggered across surfaces 1 and 2

512/ Ribbons

Threat score 21

Convenience Group Feather Friendly

DIY tape

1/8” white squares, spaced 2” on center

Threat score 23

Arnold Glass

Sample 8-F 12  ORNILUX mikado mono 12mm

Tested with background

12mm laminated made of:

4mm Float mikado (face 2) / 0,76mm PVB / 4mm Float /

0,76mm PVB / 4mm Float mikado (face 5)

Threat Score 36  Trials=83

Tested in 2012 without background, with random result LEED score might need to be restricted to installations like balconies, where light on surface ½ is asymetric; would not apply for freestanding handrails or glass walls

14 Prototypes, some now commercially available

Including

ORNILUX mikado UNO // U-Value 1,0

Outside: 6mm Float mikado (to face 2)

Spacer: 10mm Argon

Inside: 8mm laminated 2x4 Float (0,76mm PVB) N10 (face 3)

Alternative low-E coating - with 70% light

transmission can be used as light solar control

threat score 26 trials 98

19-S13

ORNILUX mikado mono - laser I

4mm Float with lasered surface (face 1)

(face 1 = bird approach side)

on demand HJ Arnold

threat score 55 	Trials: 80

20-S13

ORNILUX mikado mono - laser II

4mm Float with into glass lasered structure (face 1)

(Face 1 = bird approach side)

on demand HJ Arnold

threat score 58 	Trials: 	84

Ferro

Three more or less untestable prototypes

Guardian

Four visible pattern samples – possibly commercially available frit patterns?

PPG

Samples arrived at the very end of fall – 2 prototypes and various controls